Minutes of the opening of Mirror’s box: MC curved mirror C03004+C03006

Place and date:   Cascina , Monday March 17th 2003

Conditions of operation:

Operator: M. Punturo, help: C.N.Man

Opening of the metallic box under air flow in clean room:

##### Cleaning and air gun flowing of metallic box

Unscrewing 4 screws.

Removing of upper cover

Visual inspection of Plane face

Removing of mirror

Visual inspection of curved face of the mirror hold by hand

Positioning of the mirror in the Perugia box (cleaned in ultrasonic device and air flowed), curved face side downwards, the arrow facing the reference mark on the teflon.

Closing of the teflon box

Turning the curved face upwards

Last visual inspection before closing with metallic plate

## Number of persons during the opening:  2 (M.Punturo, C.N.Man)

Observations:

##### Plane face: no visible defects, no visible particles

Curved face: many small visible “particles” (about 20) of size up to microns , the closest one is  1 cm from the center (corresponds to defects on substrate see Lyon’s characterization)

Air gun flowing did not change anything.

##### System Manager Optics	C.N.Man	approved

##### Thermal Noise responsible	M.Punturo	approved

Suspension of last stage responsible

## Others